## Slide 1: Aspects of Fused Silica Suspensions in Advanced Detectors
Geppo Cagnoli
gianpietro.cagnoli@utb.edu
University of Texas at Brownsville and TSC
LIGO, Hanford –Feb. 2nd 2011

## Slide 2: A bit of history
Braginsky first work 1993
First suspension test 1999, Glasgow
First suspension on GEO600 2000
First laser pulling machine 2005

## Slide 3: Fused silica properties
It’s resistant to longitudinal stress
It’s soft
Low thermal expansion
Positive dE/dT
Low loss
Physical properties do not change after melting
G. Brambilla, Nano Letters 9 (2) 831, 2009
Young’s modulus is about 72 Gpa = 1/3 of steel value
Softness is important for thermal noise:
Q is proportional to jE
Softness is important for the vertical bouncing mode:
for LIGO fvert ~ 10 Hz

## Slide 4: Linear thermoelastic effect
FIBRE
Asymmetric thermal fluctuations across the fibre are responsible for the thermoelastic noise
Thermal expansion transforms thermal fluctuations in strain fluctuations
PSD of pendulum noise depends also on the characteristic time t heat takes to cross the fibre
M. Alshourbagy et al., Class. Quantum Grav., 23 (2006) S277
Thermoelastic damping is so precise that it can be used to measure thermal and mechanical properties of materials.
Here a crystalline Si fibre is under measurement

## Slide 5: Non linear thermoelastic effect
P
dT
Strain fluctuations are coupled to thermal fluctuation through the term b=1/E·dE/dT, too
A permanent static strain should be already present
Amazingly, b > 0 in fused silica:
  Thermoelastic fluctuations can be cancelled !!
IT HAS NOT BEEN VERIFIED
BY AN EXPERIMENT YET!!

## Slide 6: Mechanical losses
Mechanical losses are expressed in terms of loss angle j
At each resonant mode j is exactly Q-1.
t

## Slide 7: Losses in fused silica
F. Travasso et al., Mat. Sci. Engineering A, 521-522 (2009) 268
ADWP
Relaxation model
Surface effect +
other relaxations (?)
F. Travasso et al., Mat. Sci. Engineering A, 521-522 (2009) 268
Frequency dependence

## Slide 8: The Asymmetric Double Well Potential model
Silica smallest structure
Tetrahedras twist  modulus defect
The twist has a ADW potential
The transition time t depends on V, D and temperature
Distribution of Vs and Ds

## Slide 9: ADWP in coatings

## Slide 10: Virgo + monolithic suspensions
Silica fibres haves been pulled with the CO2 laser machine
  Developed in Glasgow
  Modified for Virgo by the Firenze Group: Matteo Lorenzini, Francesco Piergiovanni and Filippo Martelli
M. Lorenzini, Class. Quantum Grav. 27 (2010) 084021

## Slide 11: Dynamics of the suspension
3-segment model
  Created for suspension modeling
  It replaces the elastic beam equation method
  Thermal noise calculations possible
F. Piergiovanni et al., J. Phys. Conf. Series, 228 (2010) 012017
Mark Barton
G060086-00-D

## Slide 12: 3-segment vs FEA
The comparison has been made on fibres with Gaussian shape neck
F. Piergiovanni et al., J. Phys. Conf. Series, 228 (2010) 012017
Different neck profiles
Suspended mass. Moment of inertia I and C.o.M. position can be changed

## Slide 13: The bending point machine
We have developed a machine able to detect the bending point in FS fibres with a precision of 0.1 mm
The machine measures the vertical bouncing and the violin mode frequencies (as done in GEO600) for a full characterization of each fibre
F. Piergiovanni et al., J. Phys. Conf. Series, 228 (2010) 012017
MOVIE

## Slide 14: The optimal fibre shape
The optimal shape is the dumbbell
Thermoelastic noise is cancelled at the thick ends whereas the thinner part makes the bouncing mode low and violin mode high

## Slide 15: The problem of the fibre shape
Speed ratio fixes the diameter of pulled fibre but:
  At the beginning of pulling other effects are relevant
  If the fibre is pulled at constant speed the profile comes out with a neck thinner than the middle fibre diameter
  Two approaches: 1) more physics; 2) try out speed functions
M. Lorenzini, Amaldi 2009
F. Piergiovanni, private communication

## Slide 16: Suspension Creep
This phenomenon was address in Virgo for the steel suspensions
Creep occurs in wires and in blades
Creep microscopic events:
  The length of wires suddenly increases by 10-10 m or less
  The actual displacement of the mass depends on its transfer function
Length increase qL
First transfer function: wave propagation
Second transfer function: mass dynamics

## Slide 17: Creep in hydroxide-catalysis bonding?
FS fibres are known to have the creep regime overlapped with the rupture of material
Hydroxide-catalysis bonding may have creep due to a non-homogeneous curing of bonding
A direct measurement has been proposed:
  Not on suspended masses because of their low-pass filtering transfer function

## Slide 18: Proposed activity for aLIGO
Investigation on creep noise
  Shear stress due to mirror weight and thermal gradient due to thermal compensation may cause creep in the silicate bonding layer
  Previous works have searched for indirect evidence of such noise (violin modes amplitude monitoring) B Sorazu et al 2010 Class. Quantum Grav. 27 155017
  Direct detection is proposed here
Relevance for aLIGO
  Minimizing the risk of having creep noise from bonding
  A test for thermal compensation

## Slide 19: Direct measurement of creep noise
Measurement done on samples
  Test mass is pulled by its own weight  “slow” motion
  Low mass ear moves very fast when tension is released
  Vacuum conditions to avoid possible effect of air
  F-P cavity to detect events of magnitude 10-12 m
COURTESY OF GLASGOW
F-P CAVITY
100×2 N
Heat
FREQUENCY
STABILIZED
LASER